Polarization decoupling method

ηTotal=ηkinetic+ηohmic+ηproton+ηmass transport#1

Total cell overpotential is determined by a sum of various cathode overpotentials as shown in Eq. 1. Kinetic, ohmic, catalyst layer proton, and mass transport overpotentials are considered.

Determination of kinetic overpotential

From the Bulter volmer equation;

j=j0expαnFηRT-exp-1-αnFηRT#2

Where:

- j : net current density (A/cm2)

- j0 : exchange current density (rate at which forward and reverse rxn are equal at equil.)

- α : charge transfer coeff

- n : no. of electrons transferred

- F : Faraday const

- R : gas const

- T : Temp in Kelvin

- η : Overpotential (kinetic)

An assumption of a large negative overpotential (cathodic ORR) reduced Eq. 2 to Eq. 3

ηkin=a+blnj#3

Total overpotential, obtained using Eq. 4 and 5, is plotted against the current density, j. The slope and intercept of the linear region at low current density was used to estimate the kinetic contribution to the total overpotential.

ηTotal=Ecell-Erev#4

Erev=1.23-0.0009T-298+2.303RT4FlogPH2PH2,ref2PO2PO2,ref 2#5

Determination of ohmic overpotential

ηohmic=HFR *J#6

Ohmic overpotential is calculated by the product of the high frequency resistance (HFR) and the corresponding current as will be shown in the example calculation in section #.

Determination of catalyst layer proton transfer overpotential

Under H2/N2 flow conditions, EIS measurements of the catalyst MEA depict a characteristic 45° region followed by a linear region at lower frequency. The distance between the x-axis intercept of the experimental result and the x-axis intercept of the near-vertical linear region is used to determine the proton transfer resistance.

ηproton=3*R#7

CN BM

HFR+EIS

Ohmic resistance

Kinetic Overpotential Calculation

O2 1.5 bar BP

O2 0 bar BP

Air 1.5 bar BP

Air 0 bar BP

KB BM

HFR+EIS

Kinetic Overpotential Calculation

O2 1.5 bar BP

O2 0 bar BP

Air 1.5 bar BP

Air 0 bar BP

VC Polyol

HFR+EIS

Kinetic Overpotential Calculation

O2 1.5 bar BP

O2 0 bar BP

Air 1.5 bar BP

Air 0 bar BP

AB Polyol

O2 1.5 bar BP

O2 0 bar BP

Air 1.5 bar BP

Air 0 bar BP

Durability Decoupling

CN BM O2

30k

75k

CN BM Air

30k

75k

KB BM O2

30k

75k

KB BM Air

30k

75k

VC Polyol O2

30k

75k

VC Polyol Air

30k

75k

AB Polyol O2

30k

75k

AB Polyol Air

30k

75k

CN Polyol O2

BOL

30k

75k

CN Polyol Air

BOL

30k

75k

KB Polyol O2

BOL